## Slide 1: Weekly meeting
David Restrepo, Santiago Garcia Botero
* Department of Mechanical, Aerospace, and Industrial Engineering. The University of Texas at San Antonio
FFT based crystal plasticity
february 2026

## Slide 2: FFT based crystal plasticity
Introduce a homogeneous reference stiffness usually isotropic). Define the polarization stress:
Then
Plug into equilibrium:
This is now a homogeneous operator applied to , driven by a “source” term .
Periodic heterogeneous elasticity on an RVE

## Slide 3: FFT based crystal plasticity
We solve on a periodic cell with heterogeneous stiffness . Unknown displacement , strain , stress .
Kinematics and constitutive law:
Equilibrium (no body forces):
with periodic fluctuations and a macroscopic loading constraint
where denotes volume average.
Periodic heterogeneous elasticity on an RVE

## Slide 4: FFT based crystal plasticity
For periodic fields, use discrete Fourier series. Let denote Fourier coefficients. Then
Since is constant,
Therefore for all nonzero modes:
and enforce .
Computationally: compute in real space, FFT to , multiply by , inverse FFT to get .
Why FFT appears

## Slide 5: FFT based crystal plasticity
For isotropic with Lamé constants , define wavevector and unit direction .
The reference equilibrium operator reduces to the acoustic tensor
and its inverse has closed form
Given (a symmetric tensor), define
then the strain update is
At , set .
That’s your in constructive form.
Explicit spectral Green operator

## Slide 6: FFT based crystal plasticity
On an grid, the Fourier mode indices are integer frequencies . The choice of wavevector encodes the discrete derivative operator.
Continuous/spectral derivative (common baseline):
Finite-difference-compatible derivative (better near discontinuities):
You then use or to build . This choice changes the discrete compatibility/equilibrium enforcement and can dramatically improve convergence and reduce Gibbs oscillations in high-contrast RVEs.
Continuous vs discrete wavevector and why it matters

## Slide 7: FFT based crystal plasticity
Basic algorithm

## Slide 8: FFT based crystal plasticity
Convergence depends on contrast and reference medium

## Slide 9: FFT based crystal plasticity
For EVP, the stress is no longer simply . Instead you typically use an additive split:
A local constitutive update provides, at each voxel:
The global equilibrium problem is still enforced spectrally, but now each outer load increment involves an inner loop that alternates: real-space constitutive update ↔ Fourier-space equilibrium correction.
That’s EVPFFT in one sentence: local nonlinear material, global spectral equilibrium.
Elastic–viscoplastic extension

## Slide 10: FFT based crystal plasticity
FFT micromechanics solves equilibrium on periodic grids by turning the PDE into the Lippmann–Schwinger convolution equation, which becomes an algebraic multiplication in Fourier space.
Accuracy hinges on: the Green operator , the wavevector discretization (continuous vs FD-compatible), and correct handling of the zero mode.
Speed hinges on: reference medium choice, iteration strategy (fixed-point vs Anderson vs Krylov), and implementation details (batched FFTs, preallocation, GPU).
Takeaways and what controls accuracy + speed

## Slide 11
Any questions ?
Thank you